## Slide 1
BERGER TEXTURES

## Slide 2
BERGER TEXTURES
LUXURY
ECONOMY
SUPER LUXURY

## Slide 3
TOOLS REQUIRED
PUTTY MIXER
PUTTY BLADE
STEEL TROWEL
PLASTIC TROWEL
SCRAPERS
HOPPER GUN
DESIGNS ROLLERS & TOOLS
FOAM TAPE

## Slide 4
Popular & preferred grooved finish texture
Formulated with modified acrylic emulsion & reinforced with quartz – to stand with humidity, rain & variable climates.
Tough groove finish
Can be applied on fresh plastered or weather beaten surfaces For Exterior
BERGER RUFF N TUFF
SCRATCH

## Slide 5: Solvent Dilution ratio Coverage Drying Time Finish/Shades
Potable Water
Upto 3% (v/v) water for better workability
1.6 – 4.5 Sqft / kg / coat (depend on variants)
Surface dry - 30 minutes
Hard Dry: 12- 16 hours
Matt / Off white
30 KG drum/ bag; Variants – Fine, Regular, Standard, High Build
Trowel
12 months in drum packing; 6 month in bag / 2 -3 hrs of thinned material
Pack size/ Variants Application tools
Shelf life / Potlife
BERGER RUFF N TUFF
SCRATCH

## Slide 6
Direction of use
Primer application – apply 1 coat of WC exterior primer/Seal-o-prime and allow it for 4-6hrs
Texture application – Apply 1 coat of Ruff ‘n’ Tuff- Scratch with trowel and allow it to dry for 16 – 18 hrs Top coat – Apply 2 coats of Berger Weathercoat (Longlife, Antidust, Glow) as finishing coat.
Recommended Variants
Fine ( 0.8 – 1 mm): | recommended for very smooth surfaces | 
Regular (1.2 – 1.5 mm): | recommended for smooth surface | 
Standard (2 – 2.5 mm): | recommended for medium rough surface | 
High build (3mm +): | recommended for rough surface | 
BERGER RUFF N TUFF
SCRATCH

## Slide 7
SCRATCH
PRODUCT | DILUTION | COVERAGE | NO OFCOATS | TOOLS | MATERIAL COST
Scratch Fine | 3-5% of fresh water | 3 -3.5 Sq.ft./Kg/Coat | 1 | Trowel | 15/Sq.ft
Scratch Regular | 3-5% of fresh water | 2.5 Sq.ft./Kg/Coat | 1 | Trowel | 19/Sq.ft
Scratch Standard | 3-5% of fresh water | 2.5 Sq.ft./Kg/Coat | 1 | Trowel | 19/Sq.ft
Scratch Hi-Build | 3-5% of fresh water | 2-2.5 Sq.ft./Kg/Coat | 1 | Trowel | 20/Sq.ft
RUFF N TUFF

## Slide 8
RUFF N TUFF SCRATCH SITE AT KOZHENCHERRY & CHAKKUVALLY DONE BY MR. LALU

## Slide 9
RUFF N TUFF SCRATCH SITE AT THIRUVALLA DONE BY MR. SHIVAKUMAR

## Slide 10
BERGER RUFF N TUFF
PEARL
Elegant BUBBLE & spattered finish texture
All weather durability Excellent durability, long lasting
Can be applied in Interior & Exterior

## Slide 11
Potable Water
3 ~ 5 % (v/v) water for better workability
5 ~ 8 Sqft / kg / coat
Surface dry – 1 hr
Hard Dry: 16 ~ 18 hours
Matt / White
30 KG drum
Hopper spray gun
12 months in drum packing / 2 -3 hrs of thinned material
Solvent Dilution ratio Coverage Drying Time Finish/Shades Pack size
Application tools
Shelf life / Potlife
BERGER RUFF N TUFF
PEARL

## Slide 12
Direction of use
Primer application – apply 1 coat of WC exterior primer/Seal-o-prime and allow it for 4-6hrs
Texture application – Apply 1 coat of Ruff ‘n’ Tuff- Pearl with hopper spray gun and allow it to dry for 16 – 18 hrs
Top coat – Apply 2 coats of Berger Weathercoat (Longlife, Antidust, Glow) as finishing coat.
BERGER RUFF N TUFF
PEARL

## Slide 13
PEARL
PRODUCT | DILUTION | COVERAGE | NO OFCOATS | TOOLS | MATERIAL COST
PEARL | 3-5% of fresh water | 7-10Sq.ft./Kg/Coat | 1 | HOPPER GUN | 7/Sq.ft
RUFF N TUFF

## Slide 14
RUFF N TUFF PEARL SITE AT ADOOR & CHADAYAMANGALAM DONE BY MR. MANU (HI-TECH)

## Slide 15
BERGER RUFF N TUFF
DECORA
4.Decora- Plaino Super cast
1.DECORA – DHOLPUR STONE
2.DECORA – ROLLERCOAT
3.DECORA – ROLLERCAST
4.DECORA – PLAINO SUPERCAST
5.DECORA – PLAINO DESERT
6.DECORA – STUCCO ACESS

## Slide 16
BERGER RUFF N TUFF
DECORA- DHOLPUR STONE
Assorted decorative stone finish texture
Special synthetic copolymer emulsion reinforced with silica aggregates having excellent bonding properties
Excellent durability, long lasting
Covers surface imperfections & roughness Green Pro Certified

## Slide 17
Potable Water
3 ~ 5 % (v/v) water for better workability
Surface dry – 1 hr
Hard Dry: 16 ~ 18 hours
30 KG drum
Scrapper, Steel trowel, Design tools etc
12 months in drum packing / 2 -3 hrs of thinned material
Solvent Dilution ratio Coverage Drying Time Finish/Shades Pack size
Application tools
Shelf life / Potlife
BERGER RUFF N TUFF
2 ~ 2.5Sqft / kg / coat ( approx. 2 – 2.5 mm thickness)
Matt / Off -White
DECORA- DHOLPUR STONE

## Slide 18
DECORA DHOLPUR STONE
PRODUCT | DILUTION | COVERAGE | TOOLS | MATERIAL COST
DHOLPUR STONE | 3-5% of fresh water | 2-2.5 Sq.ft./Kg/Coat | SCRAPPERS, DESIGNS TOOLS etc | 18/Sq.ft
RUFF N TUFF

## Slide 19
RUFF N TUFF DECORA DHOLPUR SITE AT MANAPALLY DONE BY MR. SIVAKUMAR

## Slide 20
RUFF N TUFF DECORA DHOLPUR SITE AT CHADAYAMANGALAM DONE BY MR. MANU (HI-TECH)

## Slide 21
RUFF N TUFF DECORA DHOLPUR SITE AT KOTTARAKKARA AND CHATHANOOR DONE BY MR. BIJU

## Slide 22
RUFF N TUFF DECORA DHOLPUR SITE AT ADOOR DONE BY MR. ROBERT

## Slide 23
Durable Spike textured finish
Special synthetic copolymer emulsion reinforced with quartz & marble powder offering spike like texture
Excellent durability, long lasting
Covers surface imperfections & roughness Green Pro Certified
BERGER RUFF N TUFF
DECORA ROLLERCOAT

## Slide 24
Potable Water
~ 5 % (v/v) water for better workability
4 ~ 6 Sqft / kg / coat
Surface dry – 30 mins
Hard Dry: 12 ~ 16 hours
Matt / Off -White
30 KG drum/bag
Honey comb roller
12 months in drum packing; 6 month in bag / 2 -3 hrs of thinned material
Solvent Dilution ratio Coverage Drying Time Finish/Shades Pack size
Application tools
Shelf life / Potlife
BERGER RUFF N TUFF
DECORA ROLLERCOAT

## Slide 25
DECORA ROLLERCOAT
PRODUCT | DILUTION | COVERAGE | TOOLS | MATERIAL COST
ROLLER COAT | 3-5% of fresh water | 4-6 Sq.ft./Kg/Coat | HONEY COMB ROLLER | 7.6/Sq.ft
RUFF N TUFF

## Slide 26
RUFF N TUFF DECORA ROLLERCOAT SITE AT KOLLAM DONE BY MR. VIPIN

## Slide 27
Assorted textured finish
Reinforced with quartz & aggregates Excellent durability, long lasting
Covers surface imperfections & roughness Green Pro Certified
BERGER RUFF N TUFF
DECORA ROLLERCAST

## Slide 28
Potable Water
~ 5 % (v/v) water for better workability
6 ~ 8 Sqft / kg / coat
Surface dry – 30 mins
Hard Dry: 12 ~ 16 hours
Matt / Off -White
30 KG drum/bag
Honey comb roller
12 months in drum packing; 6 month in bag / 2 -3 hrs of thinned material
Solvent Dilution ratio Coverage Drying Time Finish/Shades Pack size
Application tools
Shelf life / Potlife
BERGER RUFF N TUFF
DECORA ROLLERCAST

## Slide 29
DECORA ROLLERCAST
PRODUCT | DILUTION | COVERAGE | TOOLS | MATERIAL COST
ROLLERCAST | 3-5% of fresh water | 6-8 Sq.ft./Kg/Coat | HONEYCOMB ROLLER | 7.5/Sq.ft
RUFF N TUFF

## Slide 30
Assorted textured finish
Reinforced with quartz & aggregates Excellent durability, long lasting
Covers surface imperfections & roughness Green Pro Certified
BERGER RUFF N TUFF
DECORA PLAINO SUPERCAST

## Slide 31
Potable Water
~ 5 % (v/v) water for better workability
2.5 ~ 3.5 Sqft / kg / coat
Surface dry – 30 mins
Hard Dry: 12 ~ 16 hours
Matt / Off -White
30 KG drum/bag
Honey comb roller
12 months in drum packing; 6 month in bag / 2 -3 hrs of thinned material
Solvent Dilution ratio Coverage Drying Time Finish/Shades Pack size
Application tools
Shelf life / Potlife
BERGER RUFF N TUFF
DECORA PLAINO SUPERCAST

## Slide 32
DECORA PLAINO SUPERCAST
PRODUCT | DILUTION | COVERAGE | TOOLS | MATERIAL COST
PLAINO SUPERCAST | 3-5% of fresh water | 2-3.5 Sq.ft./Kg/Coat | HONEYCOMB ROLLER | 16/Sq.ft
RUFF N TUFF

## Slide 34: SOLITAIRE STONE / GRANITE
Natural stone & Granite like finish
Formulated with pure acrylic emulsion with natural, colored aggregates & quartz
All weather durability & resistant to mechanical damage
Possible to get single and multi color combinations Both for Interior & Exterior;
Green Pro Certified

## Slide 35: SOLITAIRE STONE / GRANITE
Potable Water
Upto 5% (v/v) water for better workability
2 – 2.5 Sqft / kg / 2 coats
Surface dry - 30 minutes
Hard Dry: 16- 18 hours
Matt / Natural Stone like color
30 KG
Trowel / Texture spray gun
12 months in drum packing / 2 -3 hrs of thinned material
Solvent Dilution ratio Coverage Drying Time Finish/Shades Pack size
Application tools
Shelf life / Potlife

## Slide 36: SOLITAIRE STONE / GRANITE (APPLICATION SYSTEM)
Direction of use
Primer application – apply 1 coat of WC exterior primer/Seal-o-prime and allow it for 4-6hrs
Joint Sealer application – to get a tile like pattern with grooves, apply 1 coat as per required shade. After 8 hrs, fix masking
tape as per the preferred size of the grooves.
Texture application – Apply smooth & uniform 1st coat of Solitaire Stone / Granite base coat by trowel & remove masking tape. Allow the base coat to dry for 16-18 hrs. Re-fix the masking tape and apply 2nd coat of of Solitaire S/G as pattern coat by hopper spray gun to get desired texture pattern. Remove masking tape in wet condition and allow it to dry for 16-18 hrs.
Clear coat – Apply 2 coats of Solitaire Acrylic Clear- Matt/Gloss (clear lacquer) with recommended dilution as finishing coat to increase longevity and avoid dust deposition.

## Slide 37
SOLITAIRE SITE AT ADOOR & THEVALAKKARA DONE BY MR. VIPIN

## Slide 38
SOLITAIRE SITE AT ADOOR DONE BY MR. LALU

## Slide 39: FLORENTINA

## Slide 41: FLORENTINA GLITTERATTI
Single & Multi –colored luxury texture with Glitter effect In 12 attractive unique shades
Combination of selected aggregate including Mica & a high quality acrylic binder
Tough & ever lasting – resist algal & fungal growth
Weather proof – suitable for adverse conditions UV resistance
Both for Interior & Exterior; Green Pro Certified

## Slide 42: FLORENTINA GLITTERATTI (TECHNICAL SPECIFICATIONS)
Potable Water
Upto 5% (v/v) water for better workability
2.5 to 3 Sqft / kg / 2 coats
Surface dry - 30 minutes
Hard Dry: 16 – 18 hours
Textured & Glittering / 12 Shades
PART A – 10 kg & PART B – 20 Kg
Acrylic trowel/ Steel trowel
24 months in drum packing
Solvent Dilution ratio Coverage Drying Time Finish/Shades Pack size
Application tools
Shelf life

## Slide 43: FLORENTINA GLITTERATI (PRODUCT PREPARATION & APPLICATION SYSTEM)
The product consists of 2 components
Part A (10 kg) – specially formulated medium
Part B (20 kg) – Natural aggregates of different colored stones and mica flakes
Preparation method
1. Pour Part A into the empty container
2. slowly add Part B into Part A
3. Mix contents thoroughly to a uniform consistency with mechanical stirrer
Direction of use
Primer application – apply 1 coat of WC exterior primer/Seal-o-prime and allow it for 4-6hrs
Joint Sealer application – to get a tile like pattern with grooves, apply 1 coat as per required shade. After 8 hrs, fix masking tape as
per the preferred size of the grooves.
Texture application – Apply smooth & uniform 1st coat of Florentina Glitteratti (FG) by trowel & remove masking tape. Allow to dry for 12-16 hrs. Re fix the masking tape and apply 2nd coat of FG as topcoat to get desired finish. Remove masking tape in wet condition and allow it to dry overnight.
Clear coat – Apply 1 or 2 coats of Solitaire Acrylic Clear-Gloss with recommended dilution as finishing coat to increase longevity and avoid dust deposition.
Recommended DFT: 1.5 – 2 mm

## Slide 44: FLORENTINA GLITTERATI TEXTURE
Dark side
Deep treasure
Electric wine

## Slide 45: FLORENTINA GLITTERATI TEXTURE
Elegant grey
White duck
Milk lake

## Slide 47: FLORENTINA SANDSTONE
High build pure acrylic resin texture body coat
incorporating natural granite chip with pearl effect.
In 12 attractive unique shades
Tough & ever lasting – resist algal & fungal growth Weather proof – Silicon additives for enhanced water repellence;
UV resistance
Both for Interior & Exterior; Green Pro Certified

## Slide 48: FLORENTINA SANDSTONE (TECHNICAL SPECIFICATIONS)
Potable Water
Upto 5% (v/v) water for better workability
2.5 to 3 Sqft / kg / 2 coats
Surface dry - 30 minutes
Hard Dry: 16 – 18 hours
Granite chip with pearl effect / 12 Shades
PART A – 10 kg & PART B – 20 Kg
Acrylic trowel/ Steel trowel & Paint brush for design
24 months in drum packing
Solvent Dilution ratio Coverage Drying Time Finish/Shades Pack size
Application tools
Shelf life

## Slide 49: FLORENTINA SANDSTONE (PRODUCT PREPARATION & APPLICATION SYSTEM)
The product consists of 2 components
Part A (10 kg) – specially formulated medium
Part B (20 kg) – Natural aggregates of different colored stones
Preparation method
1. Pour Part A into the empty container
2. slowly add Part B into Part A
3. Mix contents thoroughly to a uniform consistency with mechanical stirrer
Direction of use
Primer application – apply 1 coat of WC exterior primer/Seal-o-prime and allow it for 4-6hrs
Joint Sealer application – to get a tile like pattern with grooves, apply 1 coat as per required shade. After 8 hrs, fix masking tape as
per the preferred size of the grooves.
Texture application – Apply smooth & uniform 1st coat of Florentina Sandstone (FS) by trowel & remove masking tape. Allow to dry for 12-16 hrs. Re fix the masking tape and apply 2nd coat of FS as topcoat to get desired finish. Remove masking tape in wet condition and allow it to dry overnight.
Clear coat – Apply 1 or 2 coats of Solitaire Acrylic Clear-Gloss with recommended dilution as finishing coat to increase longevity and avoid dust deposition.
Recommended DFT: 1.5 – 2 mm

## Slide 50: FLORENTINA SANDSTONE TEXTURE

## Slide 52: FLORENTINA VINTAGE
Creates elegant finishes of trendy natural and concrete designs
Formulated with pure acrylic emulsion with silicon Available in 9 artistic designs
Tough & ever lasting – resist algal & fungal growth Weather proof – Silicon additives for enhanced water repellence;
UV resistance
Both for Interior & Exterior; Green Pro Certified

## Slide 53: FLORENTINA VINTAGE (TECHNICAL SPECIFICATIONS)
Potable Water
Upto 5% (v/v) water for better workability
3 to 5 Sqft / kg / 2 coats
Surface dry - 45 minutes
Hard Dry: 8 - 12 hours
9 artistic designs / White shade
30 KG
Roller/Brush /Trowel
12 months in drum packing / 12 hrs of thinned material
Solvent Dilution ratio Coverage Drying Time Finish/Shades Pack size
Application tools
Shelf life / Potlife

## Slide 54
FLORENTINA VINTAGE
(APPLICATION SYSTEM)
Direction of use
Primer application – apply 1 coat of WC exterior primer/Seal-o-prime and allow it for 4-6hrs Texture application –
Step 1 : Base coat – apply smooth & uniform 1st coat of Florentina Vintage- by trowel & allow it to dry for 6 -8 hrs.
Step 2 : Pattern creation coat – apply 2nd coat of FV- by trowel & use apecific design tools immediately to make design pattern
Step 3: Clear coat application – Apply 1st coat water repellent Solitaire acrylic clear- Matt with recommended dilution- by roller/brush and allow it to dry for 6 – 8 hrs
Step 4: Tinted clear coat application- Tint Solitaire Acrylic clear- Matt with specific colorants to get the desired shade. Apply it with roller. Wipe off with sponge block in the direction of the prepared pattern to get the desired finish.
Recommended DFT: 0.8 – 1.5 mm

## Slide 55: FLORENTINA SANDSTONE TEXTURE

## Slide 56: Thank you.